## Slide 1: Precursory Signatures of Rock Failure
Harsh Vora
11/16/2018

## Slide 2: ML predicts failure in stick-slip experiments
Rouet-Leduc et al., 2017:
Variance of AE energy shows strongest correlation
AI can be used to predict time to failure
Notes: But
1. they used it on pre-fractured rock and failure is a function of friction.
2. They only use knowledge of fracture energy

## Slide 3: Precursory Signatures (Lei et al., 2006)
Granite
schist
Prior to failure:
Increase in Energy Release Rate
Decline in b-values
Decline in D-values
Notes: Identify various precursors
But do not build a predictive tool

## Slide 4: Objectives
“Each parameter is a function of the temporal distance to the critical point”
“An integrated analysis of two or more parameters may lead to more effective means of predicting time of the critical point”
Quantify temporal signatures of deformation in granular rock
Can they be combined to build a predictive tool?

## Slide 5: Biaxial Experiments on Berea Sandstone
Parameter | Modeled | Experimental
UCS (MPa) | 85.05 | 95.00
Young’s Modulus (Pa) | 4.28 | 7.50
MC Cohesion (Pa) | 29.35 | 26.10
MC Slope | 0.55 | 0.49
7.75 cm
3.8 cm

## Slide 6: Method 1: Microcrack Growth
7.75 cm
3.8 cm
1
2
3
4
6
5
7
Statistical Analysis:
Standard Deviation: Measures amount of dispersion in data
Variance: Expectation of deviation from Mean
3. Kurtosis: Expectation of how outlier-prone a distribution is (similar to skewness)

## Slide 7: Results 1: Microcrack Growth
1
2
3
4
6
5
7
Potential Microcracking precursors to failure:
High Std. Deviation
High Variance
Steep Decline in Kurtosis
Steep Decline in Event Rate

## Slide 8: Results 1: Microcrack Growth
Potential Microcracking precursors to failure:
High Std. Deviation
High Variance
Steep Decline in Kurtosis
Steep Decline in Event Rate

## Slide 9: Methods 2: Fracture Energy
Elastic Energy Released during fracture growth
Ef = Energy of micro-fracture (J)
Cf = Young’s Modulus (Pa)
σcf = Peak strength at microfracture genesis (Pa)
νf = volume of microfracture (m3)

## Slide 10: Results 2: Fracture Energy
Potential Fracture Energy precursors to failure:
High Std. Deviation
High Variance
Steep Decline in Kurtosis
Steep Decline in Energy release rate
1
2
3
4
6
5
7

## Slide 11: Results 2: Fracture Energy
Potential Fracture Energy precursors to failure:
High Std. Deviation
High Variance
Steep Decline in Kurtosis
Steep Decline in Energy release rate

## Slide 12: Methods 3: Moment Magnitude
AE events follow power law frequency-magnitude relationship
N= number of earthquakes greater than magnitude M
b = slope of frequency magnitude relationship
Spatial and Temporal clustering of Microcracks

## Slide 13: Results 3: b-value
1
2
3
4
6
5
7
1
2
3
4
6
5
7
Potential Moment precursors to failure:
Decline in b-values

## Slide 14: Why does b-value change?
1
2
3
4
6
5
7
1
2
3
4
6
5
7

## Slide 15: Methods 4: Fractal Dimension
1
2
3
4
6
5
7
Correlation Integral
D is the fractal dimension,
N is the number of micro-fracture pairs
R is the radius
High D-value: Distributed Damage
Low D-value: Localized Damage
1
3
5
7

## Slide 16: Results 4: D-value
1
2
3
4
6
5
7
1
2
3
4
6
5
7
Potential Damage precursors to failure:
Decline in D-values

## Slide 17: Summary of Precursory Signatures
Microcracking Activity:
  High Variance
  High Std. Deviation
Energy
  High Variance
  High Std. Deviation
Decline in b-values
Decline in D-values

## Slide 18: Predicting Rock Failure using Neural Networks
Inputs:
Std. Deviation of microcracks
Variance of Fracture Energy
b-value
D-value
Outputs:
Confining Pressure on Rock
Axial Stress to Failure
Axial Strain to Failure

## Slide 19: Predicting Rock Failure using Neural Networks
Inputs from 0 to 50 MPa:
Std. Deviation of microcracks
Variance of Fracture Energy
b-value
D-value
Confining Pressure on Rock
Axial Stress to Failure
Axial Strain to Failure
Training: 70% of Dataset
Testing: 30% of dataset

## Slide 20: ML Result 2: Predicting Axial Stress to Failure
Success Rate = 85.7%

## Slide 21: ML Result 1: Predicting Stress to Failure
Success Rate = 72.3%

## Slide 22: ML Result 3: Predicting Axial Strain to Failure
Success Rate = 68.3%

## Slide 23: Summary
Identified statistical precursory signatures of deformation using:
  Microcrack Growth (Std. Deviation of
  Fracture Energy (Variance of Energy)
  Moment magnitude (b-value)
  Spatial Distribution of Microcracks (D-value)
Applied Neural Networks on precursory signatures to predict
  Confining Pressure on Rock (good success rate)
  Axial Stress to Failure (moderate success rate)
  Axial Strain to Failure (moderate success rate)

## Slide 24: Future Work
Collect more data?
Improve AI Network Architecture
  Try other Machine Learning techniques?
  Or optimize Neural Networks?
Applicability to real-time prediction of failure

## Slide 25: Predicting Earthquakes
Using Machine Learning

## Slide 26: Simulated Earthquakes using DEM
David Blank, personal communication

## Slide 27: Simulated Seismograms
Images to Failure
Images
Outputs:
Images to Failure
Inputs:
X-displacement
Y-displacement
Image Number

## Slide 28: ANN Performance
Images to Failure
Images
Because of Input?
Bad predictions because?
- High dependence on input
- Lack of data

## Slide 29: RNN
Treats Input as Time Series
Lower Prediction Errors than ANN
Prediction could be improved with more data
Images to Failure
Images